## Slide 1: Design and Fabrication of Battery Case with Integrated Internal Cooling Channels Using Binder Jetting Additive Manufacturing
Presenter & Lead Researcher
Henil Patel
Co-Author(s) - Amir Yahyaeian, Dr. Yue Zhou
Aerospace Engineering Department

## Slide 2
Background
[*] See references slide for all three image sources
1

## Slide 3
Introduction
Thermal Management Device
Binder Jetting Additive Manufacturing
Materials
Design of a battery case with internal cooling channels that provide active cooling
Cost efficient production method
Batter case – Stainless steel
Coolant – Water
Fabricates complex internal channel geometries
2

## Slide 4
Little is known about additive manufacturing of thermal management devices using binder jetting method
Fewer studies have been performed that analyzes the shape for the cooling channels to optimize heat transfer efficiency
Fewer studies have been performed that simulates surface roughness and porosity into its CFD data and assess the performance difference
Research Gaps
3

## Slide 5
Research Goals
Optimizing the design of internal cooling channels.
  Maximizing the surface contact between fluid and battery case walls
  Maximizing the heat transfer
Identifying the shape with best heat-transfer efficiency
  Determining factors: velocity, temperature and pressure of fluid at inlet and outlet
4

## Slide 6
Methodology Overview
CAD Modelling of battery case and cooling channels
CFD simulation using ANSYS Fluent
Optimization of the channel designs
Binder Jetting Additive Manufacturing
Curing, debinding, and sintering of green parts
Final prototype of battery case
Micro-hardness and surface roughness measurements
Simulating the impact of surface roughness
Final Technical Report & Presentation
Design & Simulation
Fabrication
Testing and Finalization
5

## Slide 7
CAD Model - CATIA
Circular Bent Curved
6

## Slide 8
CFD Simulation - Temperature
Channel Designs | Inlet Temperature | Maximum Outlet Temperature
Circular |  | 
Bent |  | 
Sideways |  | 
Channel Designs | Inlet Temperature | Maximum Outlet Temperature
Circular |  | 
Bent |  | 
Sideways |  | 
Battery Case Walls Temperature -
Best Shape - Curved Channel Design
Maximum outlet temperature of coolant
Maximum coolant contact with surface walls
Net heat transfer rate – 1148 Watts
7

## Slide 9
CFD Simulation - Velocity
Channel Designs | Inlet Velocity | Outlet Velocity
Circular |  | 
Bent |  | 
Sideways |  | 20
Channel Designs | Inlet Velocity | Outlet Velocity
Circular |  | 
Bent |  | 
Sideways |  | 
Inlet Temperature of Water -
Best Shape - Curved Channel Design
Maximum outlet velocity of coolant
Higher outlet velocity indicates increased flow rate: improved fluid contact with the surface.
Enhanced convection heat transfer
8

## Slide 10
CFD Simulation - Pressure
Channel Designs | Pressure Drop
Circular | 
Bent | 
Sideways | 
Channel Designs | Pressure Drop
Circular | 
Bent | 
Sideways | 
Best Shape - Curved Channel Design
Highest pressure drop at the outlet
High pressure (back pressure) at pt. A
Higher pressure creates more resistance to flow, causing the coolant to move slower, hence better heat absorbance.
9

## Slide 11
Binder Jetting Additive Manufacturing
10

## Slide 12
Binder Jetting Additive Manufacturing
Powder Supply Roller Build bed Binder & Printhead
Binder, Cleaner, Waste Storage
11

## Slide 13
Sintering Profile
12

## Slide 14
Binder Jetting Printed Parts
13

## Slide 15
Average Surface Roughness = 21.9
Roughness Analysis Profilometer Results
Due to Roughness: Pressure Drop ; Coolant Velocity
14

## Slide 16
Average Surface Microhardness for sintered part = 148
Range of Microhardness = 130-260 HV
Indicates Presence of Microstructural Defects
Microhardness Test
15

## Slide 17
Conclusion
Battery case designed with three internal cooling channels: circular, bent, and curved
Curved channel had maximum cooling efficiency and heat transfer rate of 1148 Watts
Fabricated battery case prototypes using cheaper manufacturing method: binder jetting
Average microhardness – 148 HV
Average profilometer roughness – 21.9
Due to surface roughness, the pressure drop and velocity decreases slightly within the channels.
16

## Slide 18
Expand prototype design to real-world application for airplane batteries
Analyze the impact of varying the sizes, diameters, and dimensions of the cooling channels
Analyze the impact of varying number of integrated cooling channels in the battery case
Optimize the cooling efficiency and pumping power consumption of the battery case
Modify the process parameters for binder jetting to obtain high-density metallic parts
Next Steps
17

## Slide 19: THANK YOU
Questions?
Henil Patel
patelh27@my.erau.edu

## Slide 20
[*] Sources for images used on slide 2
https://www.nbcnews.com/business/travel/boeing-787-battery-fire-was-difficult-control-flna1c8754339
https://www.theregister.com/2013/01/17/faa_grounds_boeing_787_batteries/
https://engtechmag.wordpress.com/2013/03/19/boeing-dreamliner-787-battery-fix-an-annotated-graphic/
References
18